Soybean extracts as green corrosion inhibiting additives to fluoropolymer coatings

Principal Investigator: Eugene B. Caldona, Ph.D., NDSU Department of Coatings and Polymeric Materials

Why the Research is Important to ND Soybean Farmers

Farmers will become acquainted with the potential of soybean derivatives to contribute to green industrial applications, offering a path to greater involvement in environmentally friendly markets and enhancing the overall value of soybean.

Research Conducted

This project explores innovative applications of soybean derivatives, expanding their market beyond traditional food products by developing cost-effective, environmentally friendly fluoropolymer coatings containing soybean extract (SE) additives. Although fluoropolymers like poly(vinylidene fluoride-co-hexafluoropropylene) (PVDF-HFP) are valued for their hydrophobicity and chemical resistance, their applications are limited by their poor surface adhesion. This study uses SE as an additive to enhance the adhesion and corrosion protection of PVDF-HFP coatings on mild steel (Figures 1 and 2a-b).

Findings of the Research

The isoflavones in SE, rich in heteroatoms and pi-electrons, significantly improve the interaction between the coating and metal surface. Even with minimal SE, the coatings demonstrated excellent corrosion resistance in a 3.5 wt% NaCl solution. Methods used included microscopy, spectroscopy, wettability assessments, mechanical evaluations, thermal stability analyses, cyclic corrosion tests, and simulation studies. Findings revealed that coating adhesion on metal was enhanced at higher SE concentrations, without compromising the thermal stability and hydrophobicity of PVDF-HFP. The coating with 0.5 wt.% SE (PHSE0.5) showed the best performance, indicating an optimal SE dispersion (Figure 2c). This SE loading provided strong adhesion without forming hydrophilic pathways that could facilitate water diffusion. This study highlights SE additives as a sustainable, economical solution for improving the performance of fluoropolymer coatings.

Benefits and Recommendations to ND Soybean Farmers and the Industry

For ND soybean farmers, this research opens new industrial markets, supporting economic sustainability and growth. By promoting the use of SE additives for coatings, further optimizing the extraction processes, and collaborating with industrial partners, farmers can capitalize on the increased profitability and market opportunities, aligning with the mission of fostering innovation and sustainability within the soybean industry.

Captions:

Figure. 1. Schematic overview of integrating soybean extract into fluoropolymers to improve adhesion and corrosion protection.

Figure. 2. (a) Experimental scheme for obtaining SE through extraction. (b) Optical image and thickness of the coated samples. (c) Tafel curves of the uncoated and coated samples after 1 (solid lines) and 7 d (dashed lines) of immersion in 3.5 wt% aqueous NaCl solution.